This addendum lists StoPowerwall branded stucco blends, and unbranded blends covered in the Sto Corp. stucco warranty program

|  | Product Name and Description | Manufacturer | Product Data | - Mix: H20 / Bag / Sand - Mix: (Time) - Mix: (Yield)1 | Code Compliance2 | Comments |
| --- | --- | --- | --- | --- | --- | --- |
| One Coat Stucco (pre-sanded) | 102 StoPowerwall Stucco Pre-Blended – a controlled blend of portland cement, fibers, graded sand, and chemical additives | Old Castle DBA Amerimix 8201 Arrowbridge Boulevard Charlotte, NC 28723 | 102 StoPowerwall Stucco Pre-Blended | - 1-1.5 gal / 80 lb - (3-5 minutes) - (10-12 ft2 at ¾ inch) |  |  |
|  | Quikrete One Coat Fiberglass Reinforced Stucco – Sanded (no. 1200-80) – alkali resistant fiberglass reinforced portland cement based one coat stucco | The QUIKRETE Companies 5 Concourse Parkway Suite 1900 Atlanta, GA 30328 | Quikrete 1200 Data Sheet | - 5.5 - 6.5 qts / 80 lb / 210-250 lb - (3-5 minutes) - (10-12 ft2 at ¾ inch) | IAPMO 455 | Refer to ICC ESR for wind loads, use on noncombustible construction and on fire-resistance rated walls |
| One Coat Stucco (concentrate) | 103 StoPowerwall Stucco – controlled blend of Portland cement, fibers, and chemical additives | Holcim US, Inc. 200 Safety Street / Highway 453 Holly Hill, SC 29059 | 103 StoPowerwall Stucco | - 5-6.5 gal / 80 lb / 200-240 lb - (3-5 minutes) - 30-40 ft2 at ¾ inch | ICC ESR 2323 | Refer to ICC ESR wind loads, use on noncombustible construction and on fire-resistance rated walls. |
|  | 103 StoPowerwall Stucco – controlled blend of Portland cement, fibers, and chemical additives | Old Castle DBA Amerimix 8201 Arrowbridge Boulevard Charlotte, NC 28723 | 103 StoPowerwall Stucco | - 4-6 gal / 80 lb / 2.5 – 3 cu. ft. (180-240 lbs) - (3-5 mintues) - 35-40 ft2 at ¾ inch |  |  |
|  | 103 StoPowerwall Stucco (Western 1-Kote Gray Concentrate) – fiber reinforced portland cement-based one coat stucco concentrate | Sacramento Stucco Company 1550 Parkway Blvd. West Sacramento, CA 95691 | Western 1-Kote Gray Concentrate Data Sheet | - 4 gal / 80 lb / 200 lb - (Minimum 5 minutes) - (30-40 ft2 at ¾ inch) | IAPMO ER 382 | Refer to ICC ESR for wind loads, use on noncombustible construction and on fire-resistance rated walls. |
|  | EZ Concentrate – portland cement-based, fiber reinforced one coat stucco concentrate | Adams Supply 2722 Logan Street Dallas, TX 75215 | EZ Concentrate Data Sheet | - 5-7 gal / 80 lb / 200 – 250 lb - (3-5 minutes) - 27 ft2 at ¾ inch | ICC ESR 2477 | Lmited to Type V Construction. Refer to ICC ESR. Refert to ICC ESR for wind loads and on fire-resistance rated walls |
| Scratch and Bronw Coat Stucco | Amerimix Fiber Scratch & Brown Stucco Concentrate (no. 745) – Portland cement based fiber reinforced stucco concentrate for scratch and brown coat applications | Old Castle DBA Amerimix 8201 Arrowbridge Boulevard Charlotte, NC 28723 | Fiber Scratch & Brown Stucco | - 4-6.6 gal / 94 lbs. / 2.5 -4 cu.ft. - (3-5 minutes) - 40-65 ft2 at ¾ inch Use 3.0-4 cu.ft. sand for brown coat |  |  |
|  | Quikrete Base Coat Stucco – Pump Grade (no. 1139-86) – flowable portland cement based stucco designed for hand and spray scratch and brown coat applications | The QUIKRETE Companies 5 Concourse Parkway Suite 1900 Atlanta, GA 30328 | Quikrete 1139 Data Sheet | - 1.5 gal / 80 lb - (2-3 minutes) - 10-12 ft2 at ¾ inch | Complies with ASTM C 9263 |  |
|  | 108 Powerwall Scratch & Brown (Western Top Gun Premium Plaster) – base coat for conventional stucco designed to be a pump grade product. | Sacramento Stucco Company 1550 Parkway Blvd. West Sacramento, CA 95691 | Top Gun Premium Plaster Data Sheet | - 2.75 – 3.25 Gal 1/3 cement/sand - 3.75 – 4.25 Gal 1/4 cement/sand - (3-5 minutes) - 40-50 ft2 at ¾ inch | Complies with ASTM C 9263 |  |
|  | 108 Powerwall Scratch & Brown (IPC Scratch & Brown) – portland cement-based stucco concentrate for scratch and brown coat applications | IPC Buidling Products 10202 Synott Road Sugar Land, Texas 77478 | IPC Building Products | - Wkblty / 94 lb / 3.25 – 3.5 cu ft - (6 minutes) - (70-80 ft2 at ¾ inch) |  |  |
|  | EZ Scratch & Brown w/fiber – portland cement-based, fiber reinforced stucco concentrate for scratch and brown coat applications | Adams Supply 2722 Logan Street Dallas, TX 75215 | EZ Scratch & Brown Data Sheet | - 5-7 gal / 80 lb / 200 – 250 lb - (3-5 minutes) - 27 ft2 at ¾ inch | Complies with ASTM C 9263 |  |

1. Yield will vary with application technique, surface conditions, substrate variances from required tolerances, and other variables that may exist.

2. IMPORTANT: ICC ESRs should be consulted concerning use, application, and limitations associated with one coat stucco products

3. Compliance with ASTM C 926 relates to conformance with mix ratio requirements. Installation and other aspects of C926 such as stucco thickness must be followed for full compliance.

4. Use of admixtures, bonding agents, air-entraiing agents, or any other additives is not permitted as they may affect properties and workability. 	                              Revised: Sept, 2021